## Slide 1
Optical Fiber Communication

## Slide 3
Fiber Fabrication

## Slide 4: Fiber Fabrication Method
Liquid-phase (or Melting) Methods
Vapor-phase Deposition (VPD) Methods
  Outside vapour-phase oxidation (OVPO) method
  Vapour axial deposition (VAD) method
  Modified chemical vapour deposition (MCVD) method
  Plasma-activated chemical vapour deposition (PCVD) method

## Slide 5
Vapor phase deposition (VPD) method

## Slide 6
Materials for Fiber Fabrication
The starting materials are halides of silica (e.g., SiCl4) and the dopants, e.g., GeCl4, TiCl4, BBr3, etc., which are purified to reduce the concentration of transition-metal impurities to below 10 ppb. Gaseous mixtures of halides of silica and the dopants are combined in vapor-phase oxidation through either flame hydrolysis or chemical vapor deposition methods.

## Slide 7
Materials for Fiber Fabrication
Glass optical fibers are made from silica.
Other materials, such as fluorozirconate, fluoroaluminate, and chalcogenide glasses as well as crystalline materials like sapphire, are used for longer-wavelength infrared or other specialized applications.

## Slide 8
Materials for Fiber Fabrication
Silica and fluoride glasses usually have refractive indices of about 1.5. Chalcogenides can have indices as high as 3. Typically the index difference between core and cladding is less than 1%. Glass containing chalcogenides can be used to make fibers for far infrared transmission.

## Slide 9
Chemical Reaction

## Slide 10
Basic Principle of Fiber Fabrication
The oxides resulting from these reactions are normally deposited onto a substrate or within a hollow tube, which is built up as a stack of successive layers. Thus, the concentration of the dopant may be varied gradually to produce the desired index profile. This process results in either a solid rod or a hollow tube of glass, which must be collapsed to produce a solid preform. Various techniques have been developed based on the above principle.

## Slide 11
Silica
Silica exhibits fairly good optical transmission over a wide range of wavelengths. In the near-infrared (near IR) portion of the spectrum, particularly around 1.5 μm (1550 nm), silica can have extremely low absorption and scattering losses of the order of 0.2 dB/km.
Such remarkably low losses are possible only because ultra-pure silica is available.

## Slide 12
Silica Glass Fiber: Fabrication
Two step process:
Fabrication of preform
Drawing fiber from the preform

## Slide 13
Preform Fabrication
Preform:
Standard optical fibers are made by first constructing a large diameter "preform" with a carefully controlled refractive index profile, and then "pulling" the preform to form the long, thin optical fiber.
The preform is commonly made by chemical vapor deposition methods.

## Slide 14
Inside Vapor Deposition
With inside vapor deposition, the preform starts as a hollow glass tube approximately 40 centimeters (16 inch) long, which is placed horizontally and rotated slowly on a lathe.
Gases such as silicon tetrachloride (SiCl4) are injected with oxygen in the end of the tube. The gases are then heated by means of an external hydrogen burner, bringing the temperature of the gas up to 1,900 K (1,600 °C, 3,000 °F), where the tetrachlorides react with oxygen to produce silica (silicon dioxide) particles. The reaction conditions are chosen to allow this reaction to occur in the gas phase throughout the tube volume.

## Slide 15
Two Techniques
Core: Ge:SiO2; Al:SiO2; P:SiO2; Ti:SiO2
Cladding: Pure SiO2
Or
Core: Pure SiO2
Cladding: F:SiO2; BSiO2

## Slide 16
Chemical Reaction

## Slide 17
Preform Formation

## Slide 18
1. Take a tube of silica glass.
2. The gaseous mixture of reactants is fed at the end of the rotating
silica tube.
3. Tube is heated by a traversing oxygen-hydrogen burner at 1600
degree centigrade
4. Resulting chemical reaction glass particles called soot is formed.
5. Thin glass layer deposited inside the glass that is cladding of certain
thickness.
6. Then for core layer start flowing required amount of GeCl4. Stop
when Ge doped core layers deposition complete.
7. Increase the temp to 2000 degree Centigrade to collapse the tube
into solid preform.
Preform Fabrication Steps

## Slide 20
The preform is placed in a device known as a drawing tower, where the preform tip is heated and the optical fiber is pulled out as a string. By measuring the resultant fiber width, the tension on the fiber can be controlled to maintain the fiber thickness.
Drawing

## Slide 22: Liquid Phase (or melting) method

## Slide 23: Liquid Phase (or melting) method
This fiber fabrication method or Technique employs conventional glass-refining techniques for producing ultra-pure powders of the starting materials, which are oxides such as SiO2, GeO2, B2O3, Al2O3, etc., which decompose into oxides during the melting process. An appropriate mixture of these materials is then melted in silica or platinum crucibles at temperatures varying from 1000 °C to 1300 °C. After the melt has been suitably processed, it is cooled and drawn into rods or tubes (of about 1 m length) of multicomponent glass.

## Slide 24: Liquid Phase (or melting) method
The rod of core glass is then inserted into a tube of cladding glass to make a preform. The fiber is drawn from this preform using the apparatus shown in the figure below. Here, the preform is precision-fed into a cylindrical furnace capable of maintaining high temperature, normally called a drawing furnace. During its passage through the hot zone, its end is softened to the extent that a very thin fiber can be drawn from it. The outer diameter of the fiber is monitored through a feedback mechanism, which controls the feed rate of the preform and also the winding rate of the fiber. The bare fiber is then given a primary protective coating of the polymer by passing it through the coating bath. This coating is cured either by UV lamps or thermally. The finished fiber is then wound on a take-up drum.

## Slide 26: Liquid Phase (or melting) method
A fiber 20-30 km long can be drawn from a preform of about 1 m length in 2-3 h. Higher pulling rates are limited by the pulling process as well as the subsequent primary Coating operation. This method of preparing fibers tends to be a batch process and hence continuous production is not possible. Continuous manufacture is possible using another technique, which is called the double crucible method. The apparatus used is shown in the figure below.

## Slide 27: Liquid Phase (or melting) method
It consists of two concentric platinum crucibles (also called a double crucible) mounted inside a vertical cylindrical muffle furnace whose temperature may be varied from 800 °C to 1200 °C. The starting material-core and cladding glasses, either directly in the powdered form or in the form of preformed rods are fed into the two crucibles separately. Both the crucibles have nozzles at their bases from which a clad fiber may be drawn from the melt in a manner similar to that shown in the figure of the Fiber-drawing apparatus. Index grading may be achieved by diffusion of dopant ions across the core–cladding interface, within the melt. Relatively inexpensive fibers of large core diameters and, therefore, large numerical apertures may be produced continuously by this method. An attenuation level of the order of 3 dB/km for sodium borosilicate glass fiber, which is prepared using this technique, has been reported.

## Slide 30: Ref links
https://www.youtube.com/watch?v=6CqT4DuAVxs
How it’s made, fiber optics
https://www.youtube.com/watch?v=HcnqD0VR7ZE
OFS multimode optical fiber manufacturing- features and highlights